ABSTRAK

Material komposit polimer konduktif berpotensi digunakan sebagai material yang mempunyai nilai konduktif listrik tinggi dan sifat mekanik yang baik. Jika dibandingkan dengan logam, material ini lebih ringan, harga lebih murah dan mempunyai ketahanan korosi yang lebih baik, namun material komposit polimer konduktif mempunyai nilai konduktivitas listrik yang rendah. Tujuan dari penelitian ini adalah mendapatkan nilai konduktivitas listrik yang tinggi, dan kekerasan yang baik material komposit polimer konduktif pada komposisi bahan pengisi konduktif 65-80 % berat (wt.%) dengan variasi ukuran partikel dan komposisi bahan konduktif dan mendapatkan parameter proses manufaktur pengecoran material komposit polimer konduktif  yang optimum. Hasil penelitian menunjukan bahwa nilai konduktivitas listrik pada pengisi tunggal nilai tertinggi terdapat pada komposisi 80%, waktu pemanasan 120 menit konduktivitasnya adalah 30,612 S.cm-1, dengan kekerasan 95,03 SHD, sedangkan pada pengisi ganda terdapat pada komposisi pengisi keduanya 10%, waktu pemanasan 120 menit di dapat nilai tertinggi 50 S.cm-1 dengan kekerasan 93 SHD.

Kata kunci: komposit, grafit, resin epoxy, konduktivitas listrik, kekerasan

ABSTRACT

Conductive polymer composite material could be potentially to be used as materials which had  good electrical conductive and good mechanical properties. When it was compared with metals, these materials were lighter, cheaper prices and have better corrosion resistance, but the electrical conductivity is low  . The purpose of this experiment was to impruve electrical conductivity and good hardness. conductive polymer composite material on  conductive filler material composition was 65-80% by weight (wt.%) With variations in particle size and composition of conductive material and it had obtained  material foundry manufacturing process parameters for conductive polymer composites were optimum. The results in this experiment showed that the value of the electrical conductivity on  single filler. highest value contained in a composition of 80%, the heating time of 120 minutes conductivity was 30.612 S.cm -1, with hardness 95.03 SHD, meanwhile the multi filler were contained in the composition of 10%, 120 minutes heating time. It had been got highest value in 50 S.cm -1 with hardness 93 SHD.

Keywords: composite, graphite, epoxy resin, electrical conductivity, hardness