ABSTRAK

Sebagai bentuk konservasi lingkungan, dapat diwujudkan dengan penggunaan material yang berasal dari serat alam ini, yaitu  menjadikan sabut kelapa sebagai serat dari  papan komposit. Serat yang tidak sedikit dalam serabut kelapa tersebut digunakan sebagai penguat dari material komposit yang menggunakan matriks polimer yaitu resin poliester 157 BQTN-EX sebagai perekat. Serat sabut kelapa yang digunakan adalah serat sabut kelapa yang menggunakan halus dan panjang. Material komposit yang dibuat dengan susunan serat secara acak dan susunan lurus. Sifat mekanik yang diteliti dari material ini adalah kekuatan tarik dan kekuatan impak. Dari hasil pengujian didapatkan kekuatan tarik dan impak optimal. Dari material komposit serat sabut kelapa dengan susunan acak dengan variasi volume 70 : 30 matriks polimer kekuatan tarik sebesar 19,638 N/mm2 dan pada variasi volume 60 : 40 kekuatan tarik sebesar 24,307 N/mm2 dan dari material komposit serat sabut kelapa dengan susunan lurus dengan variasi volume 70 : 30 matriks polimer kekuatan tarik sebesar 22,226 N/mm2 dan pada variasi volume 60 : 40 kekuatan tarik sebesar 20,701 N/mm2 Sedangkan kekuatan impaknya pada variasi volume 70 : 30 sebesar 1,0197 J/mm2 dan kekuatan impaknya pada variasi volume 60 : 40 sebesar 0,9298 J/mm2. Perbedaan susunan dan volume mempengaruhi kekuatan dari material komposit tersebut.

Kata kunci : serat sabut kelapa, resin, poliester, uji impak, uji tarik

ABSTRACT

As a form of environmental conservation, can be realized with the use of materials derived from this natural fiber, which is made from coconut husk as the fiber composite board. The fibers are not a few in the coconut fibers used as reinforcement of composite materials using polymer matrix is ​​a polyester resin BQTN 157-EX as an adhesive. Coco fiber used is the use of coco fiber is smooth and long. The composite material is made with a random arrangement of fibers and straight arrangement. Studied the mechanical properties of this material are tensile strength and impact strength. From the test results obtained tensile strength and optimal impact. Of coco fiber composite material with a random arrangement with the variation of volume 70 : 30 polymer matrix tensile strength of 19.638 N / mm2 and the variation of volume 60 : 40 tensile strength of 24.307 N / mm2 and of coco fiber composite material with a straight arrangement with variations volume 70 : 30 polymer matrix tensile strength of 22.226 N / mm2 and the variations in volume 60 : 40 tensile strength of 20.701 N / mm2 impaknya While the strength of the volume variation 70 : 30 amounted to 1.0197 J / mm2 and strength impaknya the volume variation 60 : 40 amounted to 0.9298 J / mm2. Differences in the composition and volume affect the strength of the composite material.

.

Keywords : coconut coir fiber , resin , polyester , impact test , tensile test